## Slide 1: Extracting the Planckian scattering rate of the Strange Metal PdCrO2 from Angular-Dependent Magneto-Resistance Measurements
Juan L. Santana González
Realized in:
Laboratoire des Solides Irradiés, École Polytechnique
Under supervision of:
Gaël Grissonnanche
M2 Internship Soutenance
International Centre for Fundamental Physics: Condensed Matter Track
July 2024

## Slide 2: Table of Contents
Introduction: The Strange Metal and the Planckian scattering rate
Material: The isostructural delafossites PdCoO2 and PdCrO2
Approach: Angle-Dependent Magneto-Resistance and Chamber’s formula
Experiment: Electric transport in extreme magnetic fields
Results: Preliminary conclusions and Outlook
Conclusion

## Slide 3
The conventional metal.
Nakamae et al. PRB 2003

## Slide 4
The conventional metal. What makes it strange?
Nakamae et al. PRB 2003
Daou et al. Nat. Phys. 2009
Superconductivity

## Slide 5: What does it tell us?

## Slide 6: Unknown scattering process
Electrons: 1
Phonons: not present at

## Slide 7: Universality

## Slide 8: Universality
Universal (Planckian) Scattering Rate

## Slide 9: Universality
Planckian limit for the Scattering Rate
Drude model in Quantum Materials? We want to do better

## Slide 10
Where can we find them?
Daou et al. Nat. Phys. 2009

## Slide 11
Where can we find them?
Doiron-Leyraud et. al. PRB 80, 214531

## Slide 12
Where can we find them?
Jaoui er. al. Nat. Phys. 2022

## Slide 13
Where can we find them?
Hu et. al. Nature 2017

## Slide 14
Where can we find them?
Universal behaviour?
What do they have in common?

## Slide 15
Where can we find them?
Unconventional Superconductivity

## Slide 16
Unconventional Superconductivity
Strange Metal Physics
16

## Slide 17
Unconventional Superconductivity
Strange Metal Physics
Antiferromagnetism
17

## Slide 18
Unconventional Superconductivity
Strange Metal Physics
Antiferromagnetism
?
18
Connection between Strange Metal physics and Antiferromagnetism?

## Slide 19
Antiferromagnetism
????
19
Are antiferromagnetic fluctuations giving rise to the Planckian scattering rate?

## Slide 20
20
Materials:
The isostructural delafossites
PdCoO2 & PdCrO2

## Slide 21
The isostructural delafossites
B
A
ABO2 Structure
Quasi-2D layered system, high in-plane mobility, reduced interlayer hopping
Can be metallic, semiconductor, insulating, magnetic…
Our interest:
PdCoO2 & PdCrO2

## Slide 22: Identical structure, very different resistivity:
22
Zhakina et. al.
PNAS, 2023
Zhang et. al.
Nat. Comms, 2024
PdCoO2
PdCrO2

## Slide 23: PdCoO2
23
PdCrO2
Sobota et. al.
PRB 88, 125109
Noh et. al.
PRL 102, 256404
Lechermann, Nat.Comp.Mats, 2021
Identical Fermi Surface Only difference is

## Slide 24
24
Method:
Angle-Dependent Magneto-Resistance

## Slide 25
25
C-axis electric transport in a magnetic field

## Slide 26
26
Electrons draw orbits in the Fermi surface

## Slide 27
27
vs
Electrons draw orbits in the Fermi surface

## Slide 28
28
Resistivity oscillates due to averaging of velocities along orbits

## Slide 29
29
Resistivity oscillates due to averaging of velocities along orbits

## Slide 30
30
Resistivity oscillates due to averaging of velocities along orbits

## Slide 31
31
Extracting : Chamber’s formula

## Slide 32
32
Extracting : Chamber’s formula
Grissonnanche et. al.
Nature, 2021

## Slide 33
33
Experiment:
42 Tesla
4 samples
300 L/s for cooling
13 temperatures
Largest resistive continuous magnet in the world

## Slide 34
34
Samples

## Slide 35
35
Experiment configuration

## Slide 36
36
Experiment configuration

## Slide 37
37
Experiment configuration

## Slide 38
38
Results

## Slide 39
39
Low Temperature: Great differences due to FS folding, but clean oscillations due to

## Slide 40
40
Just above AFM transition : Barely any change in PdCoO2, but quickly rises and smears oscillations in PdCrO2

## Slide 41
41
High Temperature: In PdCrO2 all features have dissappeared, PdCoO2 starts resembling the previous PdCrO2 data

## Slide 42
42
Outlook: Transport simulations

## Slide 43
43
Outlook: Transport simulations

## Slide 44
44
Conclusion
PdCrO2 : becomes very large in the region of AFM fluctuations
consistent with Planckian scattering rate
PdCoO2 : almost constant until 80K
Resemblance with PdCrO2 at high T : Fermi surface is equal

## Slide 45
45
Thank you!
PdCrO2 : becomes very large in the region of AFM fluctuations
consistent with Planckian scattering rate
PdCoO2 : almost constant until 80K
Resemblance with PdCrO2 at high T : Fermi surface is equal

## Slide 46
S1
ADMR as probe of magnetic reconstruction in PdCrO2
Hicks et. al.
PRB 92, 014425

## Slide 47
S1
Validity of the semiclassical framework in Quantum Materials
Many successes:
Description of ADMR
Description of Seebeck coefficient in
Some failures:
Strange Metals magneto-resistance dependence (H-linear)

## Slide 48
S1

## Slide 49
S1